| AIM33 INSPECTION REPORT |
| --- |
| Joint No. | COUPLER 25 | Report No. | KNDT-AIM-03-001 |
| Drawing No. | COUPLER 25-G | Joint of Interpretation | Bad fusion interface or foreign material |
| Ultrasonic Tester Serial No. | 1040103032003050211 | Transducer Serial No. | 275-K-818A / 7.5 ㎒. |
| Inspector Name | YONG HYEON, YU | Inspection Date | 2003. 10. 15 |
| Image Capture Location: Image Capture Start Point (No.1): 20mm From Right side of Electrode |
| 25-A1 | ■A □B / ■1 □2 □3 □4 / □C1 □C2 ■C3 | 25-A2 | ■A □B / □1 ■2 □3 □4 / □C1 □C2 ■C3 |
| Interpretation | Bad fusion interface or foreign material | Interpretation | Voids or foreign material |
| 25-B1 | □A ■B / ■1 □2 □3 □4 / □C1 □C2 □C3 | 25-B2 | □A ■B / □1 ■2 □3 □4 / □C1 □C2 ■C3 |
| Interpretation | No recordable indication | Interpretation | Voids or foreign material |
| KNDT Form No. PER-①-A (A4 210 297㎜) KNDT&I Co.,Ltd. |

# Text boxes

Flow

“A” Part

“B” Part

1

2

3

4

4

3

2

1

90(

C1

C3

C2

Wire

Pipe

Coupler

0mm